## Slide 1: Lecture 27
2nd Order Nonlinear Optics

## Slide 2: Potential without inversion symmetry
Electron sees different environments on the left and on the right
-U0
x
U(x)
0
The potential is asymmetric – cannot be represented by even order curve
The next order approximation
The new equation of motion is
The electron cloud is shifted

## Slide 3: Two tone field
Let us solve equation of motion in the presence of two AC fields
E(t)
We shall look for a solution
linear
second harmonic (SHG)
sum (SFG) and difference (DFG)
DC (OR –optical rectification)
We dropped higher order terms

## Slide 4: Second order susceptibilities
Combine the terms of the same time dependence
Linear motion at optical frequency
SHG
SFG
DFG
OR
Therefore, in the response of the media we have polarization terms
Second order susceptibility
SHG coefficient

## Slide 5: Special cases
Consider SFG or DFG when
This is of course nonlinear susceptibility responsible for electro-optic effect and is equal to the nonlinear responsibility responsible for the optical rectification (reciprocity). Both OR and EO effect also include motion of ions so those susceptibilities can be quite different from the SFG and DFG when all three frequencies are in optical range.
Although SFG and SHG coefficients have different frequency dependences, for the nearly degenerate SFG when frequencies are close one has
Similarly for nearly degenerate DFG when
With that, the third rank tensor of nonlinear coefficients d can be introduced
Re-write outer product as 1x6 vector
or
SHG is a special case of SFG when

## Slide 6: Tensor of nonlinear susceptibility
For different materials the coefficients are different.
UV
Blue
Mid IR
Near IR
Vis, Near IR
Vis

## Slide 7: Transmission windows of nonlinear crystals
Lasers

## Slide 8: χ(2) order of magnitude
-U0
x
U(x)
0
a0
The nonlinear terms become comparable to linear terms when the electron is about to ionize –break the bond
Therefore
Far from any resonances,
“intrinsic” or “atomic” field that binds the electron
Alternatively
The deeper is the potential well the larger is resonant frequency , although we cannot really establish the exact dependence. So, overall as increases and thus the transparency region expands the nonlinear susceptibility decreases dramatically. That is why in UV region it is only a few pm/V and in IR can be easily 100’s of pm/V

## Slide 9: SHG efficiency
Effective SHG coefficient
d
z
Fundamental wave
SH wave
Slow variable amplitudes on the wavelength scale
Nonlinear polarization at 2ω
Displacement at 2ω
Wave equation for SH wave
Dot multiply by
Substitute
Δkz -phase mismatch

## Slide 10: Solution for non-depleted pump
d
z
0
L
Assume the pump E1 is not depleted (constant)
Solution
Power density
SHG relative efficiency (W-1)
Example LiNbO3
Assume
SHG efficiency
Coherence length “free” wave and “induced” (polarization) wave get out of phase

## Slide 11: Need for phase matching
Assume
Δk (cm-1)
Efficiency
Need to use birefringence and match for positive crystal
or for negative crystal

## Slide 12: Green laser pointer

## Slide 13: Phase matching in a birefringent crystal
Consider KDP
z
x
y
no
no
ne
k
qm
x'
x'
no
y
next(q)
Dext
Dord
Phase matching angle
Dω
D2ω
Walk-off angle
Suppose the pump beam is has a diameter
Consider index ellipsoid
Maximum propagation length is which is quite short
So-called critical phase matching
Noncritical phase matching can be done using temperature
S2
β
S1
S1
S2
Lmax
w
β

## Slide 14: Effective SHG coefficient and acceptance angle
Since the only non-zero SHG coefficients in KDP are d14=dxzy and d36=dzxy we need the fundamental (pump) wave have two projections and maximize ExEy product by choosing the polarization at 45 degrees to axis x
z
x
y
no
no
ne
k
qm
x'
Eω
D2ω
S2
β
S1
Then
Problem is a relatively narrow range of acceptance angle for phase matching
Neglect walk off
For L=1cm we are constrained to

## Slide 15: Noncritical phase-matching
Now for L=1cm we are constrained to
which is quite an improvement.
Type II phase-matching
OA
Eω
E2ω
S1
S2
k
Eω
E2ω
k
OA
Fundamental wave contains both ordinary and extraordinary components
Phase matching condition

## Slide 16: Quasi-phase matching (QPM)
j is immaterial
“discretize”
Maximum is at
SHG coefficient has a sign that can be reversed
Effective SHG coefficient
PPLN-periodically modulated lithium niobate

## Slide 17: SHG in PPLN
We can use the largest nonlinear coefficient d33
Period of poling is
x
d(x)
Λ
is square wave
Use Fourier series
Equation:
kω
k2ω
kω
2π/Λ
Matching momenta
Grating supplies the momentum

## Slide 18: 3 wave interaction
Three propagating waves
signal
idler
pump
Nonlinear polarization
small
SHG terms are not phase matched and therefore neglected
Substitute into the wave equation, neglect second derivatives, and equate the terms with the same temporal dependence
signal
idler
pump
Introduce
Power densities
Photon flux densities
Introduce
d
z
0
L

## Slide 19: Photon number balance
Coupling coefficient
units
Let us find change in photon fluxes
This shows quantum character of interaction – the signal and idler photon combine into a single pump photon ,and, vice versa, pump photon splits into signal and idler photons
So, we have Manley-Rowe relation
which is also a power conservation

## Slide 20: SHG with pump depletion
If
are real
or
Power is conserved
Input photon flux
Since try
Output saturates at 100% efficiency

## Slide 21: Frequency upconversion
k1
k2
k3
Δk
We want to convert light of IR frequency ω1 into the light of visible frequency ω3 with the help of pump ω2= ω3 – ω1 . Assume that pump E2 is not depleted and Δk=0
Typically, a3(0)=0
100% conversion at L=π/2γ
γz
N1
N3

## Slide 22: Parametric down conversion and amplification
Loss
terms
Consider the case with undepleted pump
Look for the solution
Characteristic equation
As long as γ>Δk solution is
real exponential
Assume phase matching Δk=0
Photon fluxes
Note that
For γz>>1
Assume Ni (0)=0
Both signal and idler get amplified
Ns
Ni

## Slide 23: Optical parametric amplifier (OPA)
Parametric gain is rather weak
PPLN
γ~1/cm
Therefore it is preferable to make an oscillator out of it
R1
R2
Ep
Es
Ei

## Slide 24: Optical parametric oscillator (OPO)
Consider the round trip pass for signal and idler
R1
R2
Ep
Es
Ei
z
L
0
Write the relation between input and output signal and idler fields as a matrix
If after one round trip the fields are the same then one has a steady oscillation condition and the gain is the threshold gain
Here reflectivities are diagonal matrices
Nontrivial solution only if determinant is zero

## Slide 25: OPO threshold
Double-resonant OPO, round trip loss
Single-resonant OPO, round trip loss
Threshold pump power density
PPLN
If ,
Still works and is stable
Low threshold but unstable
If ,
Idler signal starts from 0
0
L
Pump
S
Idler
Signal

## Slide 26: OPO Conversion Efficiency
0
L
Pump
N
Idler
Signal
Circulating signal photon flux Ns is constant
but the pump gets depleted. Neglect loss α
Boundary condition:
Solution:
The flux of idler photons exiting the cavity
The flux of signal photons exiting the cavity
The signal and idler photons are created and decayed in equal numbers
Conversion efficiency
Use it to find

## Slide 27: OPO photon conversion efficiency
x
(Sp /Spt)-1
η
Very high conversion efficiencies (up to 80%) are possible

## Slide 28: OPO Tuning
The phase mismatching
Assume the phase matching is achieved for the degenerate case
Let us introduce
What if change some parameter x, say angle, temperature, or period of QPM structure
Now as we change x phase matching occurs for frequencies
Tuning range increases with decrease in group velocity dispersion

## Slide 29: OPO Tuning
The phase mismatching
Assume the phase matching is achieved for the degenerate case
Let us introduce
What if change some parameter x, say angle, temperature, or period of QPM structure
Now as we change x phase matching occurs for frequencies
Tuning range increases with decrease in group velocity dispersion
GVD
For example, angle
For example, angle
signal
idler

## Slide 30: Angle phase matching tuning

## Slide 31: Temperature tuning

## Slide 32: Changing the inversion period for QPM crystals

## Slide 33: Pump wavelength tuning

## Slide 34: Generation of entangled photons
Spontaneous parametric fluorescence
Quantum key distribution