## Slide 1: Lecture 28
Nonlinear Optics
(third order)

## Slide 2: Third order effects
The third (and other odd) order nonlinearities occur in all materials, whether they do have the center of inversion symmetry or not. But there are two different ways in which the material may have a center of symmetry –it allows us to explain different 3rd order effects without quantum mechanics.
(1) Each polarizable entity, (atom, bond, or molecular orbital) has a center of inversion symmetry and is represented by a symmetric potential containing only the even orders of coordinates.
-U0
x
U(x)
0
(2) Each polarizable entity, (atom, bond, or molecular orbital) does not have a center of inversion symmetry, but for each “positive” entity there is also a ”negative” entity-so while the individual dipoles at sum and differences frequencies are generated – the second order polarization terms are all zeroes.
-U0
x
U(x)
0
-U0
x
U(x)
0

## Slide 3: Three tone field
Let us solve equation of motion in the presence of three AC fields
We shall look for a solution
linear
3-rd order
2-nd order
2-nd order
3-rd order
important
Here r(l) is the right (left) entity and

## Slide 4: Third order susceptibilities I
Beat frequency
3-photon resonance
2-photon resonance
1-photon resonance
We already know the first order response
And second order response
(easy to see that second order polarizations will cancel as )
Therefore, in the response of the media we have 3-rd order polarization terms
Third order susceptibilities
Note that and at least at low frequencies
The order makes a difference

## Slide 5: Third order susceptibilities II
1-photon resonance
Let us solve equation of motion in the presence of three AC fields
Looking for the third order terms
3-photon resonance
Both two photon resonance and also beat frequency are absent – but they represent the most important effects – two photon absorption, absorption saturation and nonlinear index.

## Slide 6: Order of magnitude
-U0
x
U(x)
0
a0
The nonlinear terms become comparable to linear terms when the electron is about to ionize –break the bond
Therefore
Far from any resonances,
“intrinsic” or “atomic” field that binds the electron
Note a very strong dependence on resonance frequency – i.e. on the transparency band width. The materials that are transparent only in IR will have much larger nonlinearity, hence on should avoid comparing apples with oranges
χ(3) is a fourth rank tensor

## Slide 7: Sum frequency and 3rd harmonic generation
Consider the nonlinear polarization term
For simplicity, consider 3-rd harmonic
No factor of 6 for this case
Introduce slow variable amplitudes for fundamental and 3rd harmonic
Substituting nonlinear polarization into the wave equation and assuming no fundamental depletion
Assume phase matching
L
0

## Slide 8: What if we cascade χ(2) instead?
L1
0
χ(2)
L2
0
χ(2)
In the first crystal we generate SH
Compare it with direct process and assume
Cascaded (sequential) process is always far more efficient than direct process
In the second crystal SF

## Slide 9: Two photon absorption
Consider and . Also assume - need to include damping
Consider the imaginary part
Lorentzian
Nonlinear polarization
Substitute it into the wave question for slow amplitude
Two photon absorption coefficient
Degenerate case
Solution

## Slide 10: Why is it TPA?
Therefore we can write
Photon flux density
Two photons must be absorbed simultaneously to conserve energy
Quantum description of TPA
ħω1
ħω0
0
ħω1
“virtual
level”
ħω0
0
ħω2
ħω2
ħω0
0
ħω0
0
E1
E2

## Slide 11: Order of magnitude
(solid state)
TPA in Si
TPA in Ge-As-Te chalcogenide
glass
TPA absorption in silicon makes it less than ideal material for Si photonics – that is why Si3N4 with low TPA in the region of interest is being used

## Slide 12: Optical limiting
Used to protect sensitive detector (or eye)
Sin
Sout
Smax
For TPA

## Slide 13: Nonlinear phase shift
Now let us look at the real part of . Consider again the degenerate case
There are two physically distinct mechanisms
The first term corresponds to off-resonant TPA – it is just a Lorentzian that peaks in the vicinity of TPA resonance. This term is a nonlinear phase delay, hence nonlinear index
Quantum picture
ħω0
0
ħω1
ħω0
0
ħω1
“virtual
level”
ħω0
0
ħω2
,
ħω2
“virtual
level”
The energy of 2 photons is not sufficient to ensure permanent absorption – photon energy get transferred to the matter (“ a spring”) but then released back to the photons – after a short delay, i.e. phase shift
ħω0
0
“virtual
level”
Δt
ħω0
0
ħω2
ħω1
ħω0
0
ħω0
0
ħω2
ħω1

## Slide 14: Nonlinear refractive index
There are two nearly equal contribution to third order polarizations from the ”virtual” TPA processes that depend on which photon gets “absorbed” first
Substitute into the wave equation
New dielectric constant
New refractive index
n2 is nonlinear refractive index
Roman-not italic!
Degenerate case –only one term
New refractive index
Overall for two fields
Cross-phase modulation
Self-phase modulation
Order of magnitude of n2

## Slide 15: The “other χ(3) ”
This term peaks near the linear absorption peak and is usually related to absorption. It usually has negative sign. It can be construed as the result of saturation. In quantum theory, when the atom (or bond) absorbs a photon it is no longer active. As the number of active atoms gets reduced, so does the susceptibility.
Near resonance we can write for the density of active atoms at lower level
τ -characteristic relaxation time
Optical power density for two waves
As long as is relatively small
Look for a solution
Then the susceptibility will also change
ħω1
ħω0
0
ħω1
ħω0
0

## Slide 16: Nonlinear index due to saturation
Nonlinear polarization
saturation
beating
Dispersion of this nonlinear index is quite resonant since both real and especially imaginary part of linear susceptibility are resonant
Since

## Slide 17: Dispersion of nonlinear index
β
n2
n2
Nonlinear absorption
β
n2
Normally we operate below 0.5 ω0 – below half-bandgap to avoid TPA

## Slide 18: Dispersion of nonlinear index
Si
GaN
Diamond

## Slide 19: Table of nonlinear indices

## Slide 20: Typical ranges of values of n2

## Slide 21: Four wave mixing
Similar term occurs in TPA nonlinearity
Pump
Signal
Idler
FWM is a third order parametric process in which two pump photons get transformed into signal and idler. The difference from the second order parametric amplification and generation is that all four photons have comparable energies (frequencies)
ω
ω1
ω3
ω2
Δω
Δω
The last two terms present a grating of with period of both refractive index and absorption.
This grating oscillates at frequency . The grating scatters wave
When multiplied by , the third term engenders nonlinear polarization at frequency but the last term generates nonlinear polarization at frequency , Similarly, scattering
off the third term generates polarization at frequency . Those are FWM terms

## Slide 22: Phase matching in FWM
So, assuming no pump depletion
Phase mismatch
kp
Δk
kp
ki
ks
GVD
Coherence length
Assume fused silica
Optical fiber near 1550nm
n2
z
0
L

## Slide 23: Coupled wave equations
Parametric gain
Consider fused Silica optical fiber
But coherence length is 800m so
Solution
The same as for
the second order parametric amplification
signal
idler

## Slide 24: Wavelength conversion via FWM
Pump
Signal
Idler
L=10km
L=1.5cm

## Slide 25: Wavelength conversion via Cross Phase modulation (XPM)

## Slide 26: Phase conjugation with degenerate FWM
Two counter propagating pumps
A signal
Nonlinear polarization
will include the term
Since and assuming undepleted equal power pumps
0
L
z
This polarization engenders a new wave, propagating in the reverse direction –z,
The propagation equation for it is
Obviously wave 4 couples back into wave 3
So the coupled equations are

## Slide 27: Phase conjugation
solution
Boundary conditions
We are interested in
Both signal and phase conjugate signal get amplified and if oscillation may occur ..
Consider light propagating through the medium with index n(z)
Signal at 0
n(z)
0
Signal at L
Conjugate signal at L
Conjugate signal at 0
Complete time reversal
All the perturbations of index are removed. Dispersion is compensated

## Slide 28: Phase conjugation-applications
Normal mirror
Wave front
diverging
Wave front
diverging
Wave front
diverging
PC mirror
Wave front
converging
PC mirror
The PC light will travel back and converge light at the source thus cancelling all the aberrations and index changes due to turbulence

## Slide 29: Digital phase conjugation

## Slide 30: Self-focusing
2w0
S
2w0
n(r)-n0
r
n2
L
Gaussian beam
Ray trajectory equation

## Slide 31: Self trapping
zsf
z
2w0
Self-focusing length
Self-focusing angle
Diffraction (divergence) angle
Effectively, convergence angle is
Critical power for convergence and eventual trapping

## Slide 32: Measurement of n2 Z-scan