## Slide 1: Lecture 29
Planar and Channel waveguides

## Slide 2: Planar waveguide
Slab waveguide
core
cladding
Maxwell equations
One can have two independent modes
Transverse electric (TE) Ez =0
Transverse magnetic (TM) Hz =0
E
H
E
H

## Slide 3: TE Modes in planar waveguide
Substitute into the wave equation
Transverse wave vector
Solution
Solution is confined in the region 1 (core) hence kx1 is real
Due to symmetry or
So there are two possible solutions inside the core
In the cladding the field decays exponentially
In-plane magnetic field
E
H

## Slide 4: Eigen modes
Boundary conditions
Continuous Ey
Continuous Hz
Even modes
Odd modes
Divide
Introduce dimensionless variables
u
v

/2
3/2 
w1
w2
Introduce normalized thickness

## Slide 5: TE modes-examples
TE1
Hx
Hz
Ey
neff=2.83
TE1
Ey
Hx
Hz
neff=1.57
Si
SiO2
n1=3.47
SiO2
n2=1.45
n2=1.45
TE0
Ey
Hx
Hz
neff=3.31
λ=1550nm
a=600nm
Si3N4
SiO2
n1=2.01
SiO2
n2=1.45
n2=1.45
TE0
Ey
Hx
Hz
neff=1.89
λ=1550nm
a=800nm

## Slide 6: TM Modes in planar waveguide
Inside the core
In the cladding
In-plane electric field
E
H
Continuous Hy
Continuous Ez
Even modes
Odd modes
Divide
Normal E-field
Discontinuity at the interface

## Slide 7: TM modes –examples
Si3N4
SiO2
n1=2.01
SiO2
n2=1.45
n2=1.45
TM0
Hy
Ex
Ez
neff=1.86
TM1
Hy
Ex
Ez
neff=1.52
λ=1550nm
a=800nm
TM0
Hy
Ex
Ez
neff=3.24
TM1
Hy
Ex
Ez
neff=1.49
Si
SiO2
n1=3.47
SiO2
n2=1.45
n2=1.45
λ=1550nm
a=600nm

## Slide 8: Effective index
Introduce effective index
Cut off
Cut off
Dispersion curves

## Slide 9: Group velocity and group index
Group velocity
Group index
Why
TM0
TE1
TM1
TE0
n1
n2
TE0
TM0
TE1
TM1
n1
n2
n2
n1
TE0
TE1
θ
θ
β
n1k0
q

## Slide 10: Power flow and effective thickness
Consider TE wave
Power density
Time averaged power density
Since is 90 degrees out of phase with
Power density per unit width
Introduce the effective thickness then
Also introduce confinement factor
a
teff
E
H

## Slide 11: Effective thickness and confinement factor
Si
SiO2
n1=3.47
n2=1.45
1550nm
a
a/2
1550nm

## Slide 12: Slab waveguide that is not symmetric
n2 substrate
n1
n3 <n2 cover (often the air)
n2 substrate
n1
n3 <n2 cover
Substrate mode
n2 substrate
n1
n3 <n2 cover
Guided mode
n2 substrate
n1
n3 <n2 cover
Radiating mode

## Slide 13: Dispersion in planar waveguide
ω
β
n3ω/c
n2ω/c
n1ω/c
TE1
TE0
TE2
Guided
modes
Radiation
modes
Substrate
modes
Forbidden region
Even the fundamental mode TE0 has a cut-off!

## Slide 14: Channel waveguides
anti-resonant reflecting optical waveguide

## Slide 15: TE Modes in channel waveguides
TE0
TE01
TE10
|E|
|S|
800nm x 500nm ridge waveguide Si on SiO2 (1.55um)
In Channel waveguides you cannot separate pure “TE” and “TM” modes – there is always a longitudinal component of the field, so “TE” and “TM” simply means “almost horizontal” or “almost vertical” polarization

## Slide 16: TM Modes in channel waveguides
TM0
TM01
TM02
|E|
|S|
800nm x 500nm ridge waveguide Si on SiO2 (1.55um)

## Slide 17: Effective index and GVD
Zero GVD
800nm x 500nm ridge waveguide Si on SiO2 (1.55um) TE0 wave

## Slide 18: TE Modes in channel waveguides
TE0
TE01
TE10
|E|
|S|
2000nm x 1000nm ridge waveguide Si3N4 on SiO2 (1.55um)

## Slide 19: TM Field in channel waveguides
TM0
TM01
TM02
|E|
|S|
2000nm x 1000nm ridge waveguide Si3N4 on SiO2 (1.55um)

## Slide 20: Effective index and GVD
No Zero GVD
2000nm x 1000nm ridge waveguide Si3N4 on SiO2 (1.55um)

## Slide 21: Reciprocity and orthogonality
subtract
add up
Conjugate and switch 1 and 2
reciprocity
Consider two modes
Integrate over dxdy

## Slide 22: Orthogonality and normalization
TE wave
TM wave
Expand fields into the modes
Some simplifications
Power along the direction of propagation in each mode
Normalization
In weak waveguides
Dimensionality

## Slide 23: Reciprocity and time reversal
add
Subtract
switch 1 and 2
reciprocity
Time reversal
If we change simultaneously and the Maxwell’s equations still hold
In complex form take complex conjugate of
Therefore, implementing change does not change all the equations and reciprocity can also be written as
Integrate over the volume and use Gauss theorem
(fields vanish at infinity)

## Slide 24: Orthogonality –another look
Power along the direction of propagation
In the absence of loss
This expression should be true for any combination of A’s
Now, what if the wave propagates backward?
Add up

## Slide 25: Waveguide with perturbation
n2
n1
n3
subtract
Now consider that dielectric constant is perturbed as
and it should lead to
Integrate over the area of waveguide
TE wave
TM wave

## Slide 26: Waveguide with perturbation (amplitude change)
subtract
Now consider that dielectric permittivity is perturbed as
Integrate over the area of waveguide
TE wave
TM wave
But
Obviously, for, say absorption