## Slide 1: Lecture 34
Localized SPP

## Slide 2: Quasi-Static Regime
Consider the situation when the fields are confined within volume ~a3 and a<<λ0/n
In free space
In a small volume
a
λ0/n
Magnetic field becomes vanishingly small when the electric field is confined to sub-wavelength volumes
The field is irrotational, hence one can introduce scalar potential
The only remaining Maxwell’s equation is the Poisson equation for the electrostatics, even though the field and charge are time dependent with optical frequency
In the absence of free charges –Laplace equation

## Slide 3: Polarized sphere in the electric field
E0
z
r
θ
a
εr1
εr2
+
+
+
+
+
-
-
-
-
-
External electric field E0 induces surface charge.
The potential changes.
Electric field
But we also know that potential of a dipole is
If dipole is oriented along z
Therefore
Induced dipole is
p

## Slide 4: LSP resonance
Induced dipole is
If
even if
Self-sustained oscillations!
Therefore
p
+
+
+
+
+
-
-
-
-
-
εm<0
εd>0
Of course this can happen only at a certain frequency
LSP frequency is
For a non-spherical particle one gets
For a prolate spheroid particle l>1 and for oblate one l<1
l>1
l<1

## Slide 5: LSP excitation
E(t)
Near resonance
Introduce polarizability
It is easy to see that this is the solution of equation for a driven oscillator
Simply a collective motion of all carriers inside

## Slide 6: LSP field enhancement near resonance
Ag
On resonance, for
E(t)
“hot spot”
Au
The field enhancement and linewidth of extinction spectrum do not depend on the size of nanoparticle (as long as it is sub-wavelength).
Absorption coefficient

## Slide 7: Plasmonic colors
Gold
Color change due to pH variation on biosynthesized silver nanoparticles A: pH 2, B: pH 4, C:pH 6, D:pH 8, E:pH 10 .

## Slide 8: Energy in the LSP
Energy outside the metal
Energy inside the metal
Total energy
Energy dissipation
The decay rate of LSP is the same as the scattering rate γ in the metal – no matter what is the shape or size of the nanoparticle (as long as a<<λ)
Neglect the magnetic field

## Slide 9: Another way to look at it
Kinetic energy density:
One half of energy is contained in the kinetic motion of carriers (or one can say that energy oscillates between the kinetic energy of carriers and potential energy of the field)
Energy conservation can be written as
from which the LSP resonance condition follows.
Kinetic Inductance -wire
a
Becomes very large for small diameter
Magnetic inductance

## Slide 10: LSP resonance as a circuit
Sphere -Kinetic Inductance
a
Sphere –Capacitance
Resonant frequency
Correct value
No size dependence
Magnetic inductance
Resonant frequency
As expected in any resonator
LK
C

## Slide 11: Why do we need metal?
It follows directly from the Heisenberg’s uncertainty principle
For most of the applications in plasmonics and metamaterials we want to concentrate optical field on sub-wavelength scale…but are prevented by the diffraction limit
To see how we can beat diffraction limit …let us re-derive it from the energy conservation considerations
What if n is not a real number???

## Slide 12: Energy balance in a mode
Electric Potential”
Energy
Magnetic
“Kinetic”
Energy
E
wt=0
a
l
H
wt=p/2
a
l
UM
UE
Energy oscillates between potential (electric) and kinetic (magnetic)
v
v

## Slide 13
UM
UE
E
wt=0
a
l
H
wt=p/2
a
l
Electric
“Potential”
Energy
Magnetic
“Kinetic”
Energy
Lack of energy balance in a sub-l mode
If a<<l0/2n there is almost no magnetic field (quasi-static limit) UM<<UE –energy is not conserved
The energy will radiate because it cannot all fit into magnetic energy –this is diffraction limit!

## Slide 14
Electric
“Potential”
Energy
Magnetic
“Kinetic”
Energy
Free carriers restore balance in a sub-l mode
E
wt=0
a
l
+
+
+
H
wt=p/2
a
l
v
J
True
Kinetic”
Energy of electrons
LK=Kinetic Inductance
(inertia of electrons)
UE
UM
UK
At some frequencies w0 the balance is achieved. These frequencies are the the resonant frequencies of the Surface Plasmon Polariton Modes
If a<<l0/2n there is almost no magnetic field (quasi-static limit) UM<<UE – hence energy oscillates between electric energy and kinetic energy of free carriers

## Slide 15: Success Always comes with the price!
In the sub-wavelength metallic structures (in all three dimensions !) half of the time almost all the energy is stored in kinetic motion of electrons –where it is being lost with the decay rate 2 of the order of 1014 s-1. Therefore the rate of energy loss in truly sub-wavelength structure is always of the order of .
t=T/4
J
a<<l/2n
0
5
10
15
20
25
2.2
2.3
2.4
2.5
2.6
2.7
2.8
2.9
3
Wave number  (relative units)
Energy (eV)
Light line
“Long range SPP”
“True sub-wavelength SPP”
Here sub-wavelength simply means very large wave-vector
Notes: 15

## Slide 16: Estimate of effective loss (SRR)
Q of Drude metal structure actually gets reduced with wavelength and only starts getting better when < - THz region which is not really optics –and even then LC circuit is not a very high Q resonator!!!!!
The true sub-wavelength region where kinetic inductance dominates (plasmonics) is inherently lossy and various geometric tricks will not mitigate this loss significantly!
optics
electronics
Border wavelength w~g
(where optics – displacement current and electronics - conductivity current meet
That is why high Q resonators in electronics include:
Quartz crystals Q~106
Surface acoustic waves Q~105
/2 cavities Q~103 ….
Split Ring Resonator
Notes: 16

## Slide 17: What happens at low frequencies?
If g>>w
There is no wavelength dependence!
At low frequencies, where conductivity current dominates magnetic field can be high enough even in the sub-wavelength structures
Of course, a simple example of truly subwavelength low loss structure is an electrical transformer at 50Hz

## Slide 18: How does the loss depend on wavelength?
UE
UM
UK
Energy stored in the magnetic field (it does
not dissipate)
Energy stored in the kinetic motion of carriers (it dissipates )
Consider a wire
a
a
t
Effective loss rate
Kinetic Inductance
Magnetic Inductance
The loss rate does not depend on frequency-only the ratio of the critical (smallest) dimension to the plasma wavelength. The loss is reduced for the structures bigger than plasma wavelength. These structures are subwavelength for l>>lp

## Slide 19: Loss vs. size
Diameter a/λp
Effective Loss γeff/γ

## Slide 20: Plasmonic and loss are inseparable
Frequency (1/l)
Confinement (1/a)
1/150nm
1/50mm
Conductivity current
Free carriers
ELECTRONICS
PLASMONICS
Reactive (Displacement) current, bound carriers
OPTICS
“METAL OPTICS”
“True Plasmonic Regime” implies that a significant part of energy s stored in motion of charged carriers. This regime is inherently lossy and should be avoided if possible.
At lower frequencies one enters the “metal optics” or “nanoantenna” or “microwave” (which extends into THz and mid-IR) regime where magnetic inductance dominates. This low loss regime is highly desirable