## Slide 1: Lecture 25
Magneto-Optics and Optical Activity

## Slide 2: Time reciprocity
This arrangement does stop the light reflected from the mirror from coming back
But it does not stop the light originating on the right from going left
The reason is time reciprocity of linear, non-magnetic and lossless optics
We have a set two second order differential equations:
If we reverse the sign of time both equations will stay unchanged – hence the time reciprocity if only electric forces are considered

## Slide 3: Nonreciprocity with Magnetic field
+V
-V
v1
v2
v3
v4
If we reverse direction
-v4
-v3
-v2
-v2
End up where we have started from
E
What if we have DC magnetic field?
Lorentz Force
v1
v1
v1
v1
If we reverse direction
v1
v1
v1
We do not get back – no time reciprocity because the first derivative changes sign
B

## Slide 4: Motion In The Presence Of DC Magnetic Field
z
y
x
k
Ey
Ex
E0
+
-
B
Consider isotropic medium
e-cloud
Kx
Ky
DC Magnetic field will try to impose counter-clock-wise circular motion onto the electron therefore we consider circularly polarized light
Equation of motion:
Introduce the Larmore frequency

## Slide 5: Motion In The Presence Of Magnetic Field
Equation of motion:
B
K
K
Two projections
×j
+
Introduce
Looking for harmonic solution

## Slide 6: Susceptibility In The Presence Of Magnetic Field
B
K
K
Projections:
Circular polarization
Different susceptibilities for different helicities

## Slide 7: Dielectric constant In The Presence Of Magnetic Field
B
Dispersion curves shift left or right by Larmore frequency
0.85
0.9
0.95
1
1.05
1.1
Frequency w/w0
Dielectric constant

## Slide 8: Verdet constant
Phase shift between two circular polarizations
Verdet constant
B
L
Faraday's cell
Émile Verdet
1824-1866
Order of magnitude
V~10 rad/T.m

## Slide 9: Verdet constant of different materials
Material λ(nm) V (rad T-1)
Water 589.3 3.81
Diamond 589.3 4.68
Quartz 589.3 4.84
Light flint glass 589.3 9.23
CS2 589.3 12.3
Pr3+ -B glass 670 -70.7
Pr3+ -Al- Si glass 700 -57.6
Tb3+ - Al- Si glass 700 -62.8
Dy3+- Al-Si glass 700 -79.1
Pr3+ - P glass 700 -35.8
Tb3+ - P glass 700 -43.6
Ce3+ -P glass 500 -94.7
700 -38.4
Pure silica glass 532 4.77
632.8 3.13
785 2.58
Tb3Ga5O12 500 -218
632.8 - 134
800 -65
1300 - -20
Verdet constant is positive for diamagnetic materials and negative for paramagnetic materials

## Slide 10: Jones Matrix of Faraday’s cell
Introduce the vector in which polarization state is a superposition of right and left circular polarizations
In this basis the Faraday's cell is nothing but a retardation plate
In the xy basis then
Linearly polarized light rotates by the angle
z
y
x
k
E
E-
E+
E-
E+
y
x
E
Specific rotation

## Slide 11: Polarization rotation in permanent magnets
Quite often one uses permanent magnets made from a ferromagnetic or ferromagnetic material with internal magnetization M Then polarization rotation is
Saturation magnetization
YIG –Y3Fe5O12

## Slide 12: Dielectric constant
Therefore, tensor of dielectric constant is
Substitute into the wave equation for the circularly polarized light
What happens with a tensor of dielectric constant?
Polarization
Meaning of δ –
rotation over the length L=nλ/π
As expected

## Slide 13: Sanity check
What about the energy? Imaginary permittivity implies loss, does not it?
Displacement vector is
Displacement current is
is out of phase with E –no power dissipation
Power dissipation
The energy does not change as it should be – DC magnetic field does not change energy
So, off diagonal elements can have imaginary part and it does not mean loss
(as long as the matrix is Hermitian, i.e. )

## Slide 14: Optical isolator
B
L
B
L
E
E
45
E
Light goes through
In
Out
E
In
E
Both x and B get reversed
No light goes through!
B
x
y
B
x
y
×

## Slide 15: Optical circulator
Bidirectional transmission over a single fiber
Configuration of optical circulator. 1: Polarization beam splitter (PBS), 2: reflection prism, 3 and 6: Birefringence crystal, 4: Faraday rotator, 5: half-wave plate
Filtering with Fiber Bragg grating
R45
R45
R45
R-45

## Slide 16: Optical Activity
Two enantiomers of a tetrahedral complex.
Shells of two different species of sea snail: on the left is the normally sinistral (left-handed) shell of Neptunea angulata, on the right is the normally dextral (right-handed) shell of Neptunea despecta
Optical activity is phenomenon of circular birefringence that occurs in certain materials, called chiral that occurs without any external field. In chemistry, a molecule or ion is called chiral if it cannot be superposed on its mirror image by any combination of rotations and translations.

## Slide 17: Origin of optical activity
z
y
x
“molecule”
E
+
-
H,B
J
Dipole along x direction
According to Lenz rule
z
y
x
“chiral molecule”
E
+
-
H,B
J
Helical current – charges move along y as well
E
+
-
Response of chiral entity

## Slide 18: Optical activity
But
Consider wave propagating along z direction, then
90 degrees rotation
Gyration tensor
Response of a chiral entity
Sign changes with direction of propagation – indicates reciprocity
Compare with Faraday effect
Sign does not depend on direction of propagation-only on the direction of magnetic field –no reciprocity
Gyration vector
(dimensionless)

## Slide 19: Polarization rotation
Phase shift between two circular polarizations
Optical rotary power
Rotation angle
Rotation is reversed for backward propagation – no isolation!
Very strong dispersion
Just as for Faraday effect

## Slide 20: Optically active crystals