## Slide 1: Lecture 26
Acousto-optic effect

## Slide 2: Effect of Strain
e-cloud
Ky
Kx
-U0
x,y
U(x,y)
0
Apply Strain
e-cloud
Kx
Ky
-U0
x,y
U(x,y)
0

## Slide 3: Strain tensor
x
y
v(x,y,z)
u(x,y,z)
Tension/Compression
u, v, and w are the displacements from equilibrium position along x, y and z respectively.
Shear

## Slide 4: Changes in index ellipsoid
Introduce one-index notation for the strain tensor
Original index ellipsoid
Introduce 6x6 strain optic tensor P
Changes in the impermeability tensor
New index ellipsoid

## Slide 5: Examples of strain optical (photoeastic) tensor
In Fused Silica
Isotropic media
Just two independent components
In water
Impermeability tensor
Medium becomes uniaxial
Consider longitudinal acoustic wave propagating along z direction in isotropic medium

## Slide 6: Examples of strain optical (photoelastic) tensor
In LiNbO3
8 independent components
Ellipsoid equation
Medium becomes biaxial with principal axes rotated in yz plane
Consider transverse (shear) acoustic wave propagating along z direction and polarized along y direction in LiNbO3

## Slide 7: Photoelastic coefficients at λ=632nm

## Slide 8: Light diffraction on acoustic waves (phonons)
Diffracted Light
0 order
-1 order
+1 order
+2 order
-2 order
Acoustic wave
L
interaction length
Light
wave
Two regimes
Raman-Nath diffraction (Multiple diffraction orders)
Bragg diffraction (Single diffraction order)
Acoustic wave
0 order
+1 order
Bragg Diffraction
Light
wave
Raman-Nath diffraction
z
L=2p/K
S,Dn
Acoustic Amplitude
and Index Change
Example: SiO2

## Slide 9: Raman-Nath diffraction
Acoustic wave produces moving refractive index grating
For thin plate (small L) phase delay is
Transmitted field is
Expand into the Fourier series using properties of Bessel function
drop
1888-1970
Incident field

## Slide 10: Raman-Nath diffraction
0-order term
+1-order term at frequency w+W
(-1)-order term at frequency w-W
k
k+
K
q1
k
k-
K
q-1
Direction of propagation
Diffraction grating
Energy and momentum
conservation
The wave-vector along x must change (a bit)

## Slide 11: Raman-Nath diffraction
k
k+
mK
qm
The magnitude of m-th maximum is determined by
0
2
4
6
8
10
0
0.2
0.4
0.6
0.8
1
If D=2.405 all the light is diffracted
If D=1.85- intensity of the 1st order reaches maximum 34%
For small D<<p/2
Diffraction efficiency into the first order
Acoustic wave intensity
Diffraction angle
Acoustic wave Power
H
Figure of merit

## Slide 12: Raman Nath modulator
Light
wave
stop
+1 order
-1 order
0 order
Acoustic wave
L
Problem:
Limited bandwidth

## Slide 13: Bragg diffraction
Wave equation without acoustic wave is
Has a solution
In the presence of acoustic wave
Obviously terms with frequencies are generated as light propagates
Acoustic wave
0 order
+1 order
Light
wave
-1 order
k
k-
k+
q
z
x

## Slide 14: Bragg diffraction
Look for the solution in the form
Am –slowly variable amplitude
Acoustic wave
0 order
+1 order
Light
wave
-1 order
k
k-1
k+1
q
z
x
Now equalize the terms with the same time dependence exp[-j(w+mW)t]
Substitute into the wave equation
These
2 will cancel out

## Slide 15: Bragg diffraction
The terms with the same time dependence exp[-j(w+mW)t]
are the terms with Am. on the l.h.s. and terms with Am+1 and Am-1 on the r.h.s.
Introduce wave vector mismatch
Obviously solution grows linearly only when Dk~0 otherwise it oscillates as sinc function. Clearly no more than a single wave vector mismatch can be equal to zero simultaneously . Let us say the very first one, between 0 and +1 order
z
qB
Bragg condition
or
Acoustic wave creates a moving multilayer reflector
Coupling strength

## Slide 16: Bragg’s Law
1862-1942
W.H.Bragg
W.L.Bragg
1890-1971
z
qB
Bragg condition
or

## Slide 17: Coupled waves equations
Acoustic wave
0 order
+1 order
Light
wave
k
k+1
q
z
x
New variables
Looking for the solution:
Characteristic equation
The determinant must be equal to zero

## Slide 18: Power balance
Boundary conditions:
Power transfer
P
1
P0
P+
z
Complete power transfer is possibly only when Dk=0
P
1
P0
P+
z

## Slide 19: Modulation efficiency and speed
z
P0
P+
L
Complete power transfer-100% modulation
Example: TeO2
for small acoustic powers
same as Raman Nath
Modulation speed: limited by the sound transit time across the beam waist w0
If

## Slide 20: Acousto-optic modulators and deflectors
By changing RF frequency one can change deflection angle
Of course there is a limit to deflection angel because eventually one cannot get good momentum matching

## Slide 21: Collinear interaction
This off-diagonal element couples extraordinary wave with ordinary wave with wavevector
mismatch
For collinear propagation
Acoustic wave
L
x
z
y
LiNbO3
H
W

## Slide 22: Acousto-optic tunable filter
Optical frequency at which the wave vectors are matched
Then at frequency
Length and power are adjusted for complete power transfer (polarization rotation) at
By changing acoustic frequency we can select optical frequency within Δν

## Slide 23: Non-collinear AOTF

## Slide 24: Acousto-optic spectrum analyzer