## Slide 1: Lecture 32
Plasmonics

## Slide 2: Metal properties
Metal dielectric constant
0.2
0.4
0.6
0.8
1
1.2
1.4
1.6
1.8
2
-200
-150
-100
-50
0
50
εr
Wavelength (μm)
0.2
0.4
0.6
0.8
1
1.2
1.4
1.6
1.8
2
0
5
10
15
20
εi
Wavelength (μm)
Metal conductivity
Plasma frequency
Metal Plasma Frequencies and Scattering Rates
gold Au 2081 THz 8.5 eV 12.31013 s-1
silver Ag 2182 THz 9.0 eV 3.2 1013 s-1
aluminum Al 3231 THz 13.2 eV 27.31013 s-1
Plasma frequency
Scattering rate

## Slide 3: Permittivity of gold

## Slide 4: Bulk Plasmons
Re-write dielectric constant
Screened plasma frequency
Neglect damping
Maxwell equation:
Transverse wave
Another solution: Longitudinal wave
Magnetic field is zero!
We can also write
Charge oscillations wave
Shifted by 90 degrees in phase
Electron density wave
Continuity equation
Current density
Works for any k!!!
No energy flow
“quasi-static wave”
E
ρ
z
z
+
+
+
+
-
-
-
Dispersion of bulk plasmons
k
ω
ωps
Goes to very large k’s –beyond diffraction limit

## Slide 5: Origin of bulk plasmons
Metal
Free Electrons
z
-
-
-
-
-
-
-
-
-
-
-
-
+
+
+
+
+
+
+
+
+
+
+
+
Qs Surface Charge
Es
Induced field
What if there is no external field, and we just move all the carriers by Δz?
S-area
Induced field
Force acting on each electron
Equation of motion
Self-sustaining longitudinal oscillations
Fs

## Slide 6: Surface plasmon
metal
dielectric
d>0
m<0
-
-
-
+
+
+
+
+
+
+
+
+
-
-
-
-
-
-
-
-
-
+
+
+
+
+
+
+
+
+
-
-
-
-
-
-
-
-
-
+
+
+
+
+
+
+
+
+
-
-
-
-
-
-
-
-
-
+
+
+
+
+
+
+
+
+
-
-
-
-
-
-
Self-sustaining surface charge oscillations
Reduction of resonance frequency is due to fringing of the field – only one half of the field actually contributes to the tangential restoring force acting upon the electrons

## Slide 7: Surface plasmon polaritons (SPP)
Surface plasmons are not pure longitudinal waves …hence they can couple with transverse electromagnetic waves – photons
d>0
m<0
metal
dielectric
x
z

Hy Ez
SPP is a TM wave propagating along the interface and evanescent in both mediums, with an interesting dispersion
Maxwell equations
E
H

## Slide 8: Surface plasmon polaritons (SPP)
Inside the metal
In the dielectric
E
H
Subtract
Longitudinal electric field
Boundary condition –continuous Ez
Effective index
When

## Slide 9: SPP dispersion
Surface plasmon resonance frequency
If the dielectric is vacuum and also then
For
Light is mostly in the dielectric
d>0
m<0
metal
dielectric
For
50% of light is in the metal
d>0
m<0
metal
dielectric
“photon -like”
“plasmon -like”
|E|2
|E|2

## Slide 10: SPP characteristics
Spatial confinement
Sub-wavelength confinement
For
Slow wave
Normal wave
Group velocity

## Slide 11: Why SPP is a slow wave?
metal
dielectric
d>0
m<0
Pointing vectors in the dielectric and metal point in the opposite directions
y
z
x
Power is
One half of the energy is in the metal and the other half is in dielectric – as they propagate in the opposite directions there is no net motion of energy
Near the SP resonance !!!
Naturally, the effective rate of the energy decay for the SP mode approaches half of the energy decay rate i.e. γ


## Slide 12: More SPP characteristics
“polarization” is “elliptical” as x and z components are shifted by 90 degrees.
d>0
m<0
metal
dielectric
In metal
In dielectric
Transverse
(photon)
Longitudinal
(plasmon)
Elliptical(polariton)

## Slide 13: Effective impedance of SPP
d>0
m<0
metal
dielectric
|E|2
Total electric field in the dielectric
Effective impedance increases with β
For
Large impedance means difficulty in coupling
Total electric field in the metal
Smaller effective impedance
η‘SPP
ηSPP

## Slide 14: Energy of the SPP
d>0
m<0
metal
dielectric
|E|2
Magnetic energy (per unit area) in the dielectric
Magnetic energy (per unit area) in the metal
Electric energy (per unit area) in the dielectric
Electric energy (per unit area) in the metal
Normalize to
In Metal
In Dielectric
Electric
Magnetic
Electric
Magnetic

## Slide 15: Potential and Kinetic Energies
Kinetic energy density:
Electric (potential) energy
Oscillates as cos2ωt
Kinetic energy
Oscillates as sin2ωt
In phase electric energy oscillating as cos2ωt
Magnetic energy oscillating as sin2ωt
Total out of phase (quadrature)energy oscillating as sin2ωt
Perfect Balance!
In phase electric
Magnetic
Kinetic
In phase electric
Magnetic
Kinetic
Photon-like
Photon-like
Plasmon-like
Plasmon-like

## Slide 16: Damping and Propagation Length of SPP
Approximately
Propagation length
Power flow
Maximum β
Typically in the visible
Gold/Air
Real β
Imaginary β
Real β for γ=0
β in units of ndωsp /c
ω/ωsp
Close to SP resonance
Silver/Air
(silver oxidizes easily)

## Slide 17: Damping and propagation length
Figure of merit
Au
Ag
neff
Au
Ag
neff
γ/ωsp=0
γ/ωsp=0.15
0.05
0.1
β in units of ndωsp /c
ω/ωsp
The maximum wavevector is limited by the damping

## Slide 18: SPP excitation
k0nd
βspp
k0n2
k0n2sinθ
n2 >nd
nd
ATR (attenuated total reflection)
θ
z
Kretschmann configuration
Resonance condition
Also works as a sensor
k0nd
k0n2sinθ

## Slide 19: Plasmonic sensing
+δn
0
20
40
60
80
Angle (deg)
0
0.2
0.4
0.6
0.8
1
R
e
f
l
e
c
t
i
v
i
t
y
δθ
n2
-200
-100
0
100
200
300
Distance (nm)
0
0.2
0.4
0.6
0.8
1
E
l
e
c
t
r
i
c
F
i
e
l
d
nm
nd
n2 >nd
nd
θ
Index change

## Slide 20: Plasmonic sensors

## Slide 21: SPP excitation

## Slide 22: SPP enhanced LED