## Slide 1: Lecture 33
Slab and Gap Surface Plasmon Polaritons

## Slide 2: SPP’s in thin metal layers
SPP1
SPP2
ωsp1
ωsp2
SPP1
SPP2
What happens when the metal is thin (less than skin depth) and two SPPs are coupled ?

## Slide 3: Slab SPP
Inside the metal
In the cladding
Same for odd mode –
cosh in place of sinh
For odd mode
Skin depth
Introduce
x
0
+a/2
-a/2
Boundary condition –continuous Ez

## Slide 4: Slab SPP
Graphic solution
Gold on glass
W=1
W=0.5
W=0.25
W=0.1
even
odd
Odd solution always has larger v than even solution. Therefore the even solution spreads more into dielectric and has lower loss than odd solution, which is well confined to the meta, therefore even solution has longer propagation range
As long as

## Slide 5: Slab SPP
odd
even
Gold on glass
odd
even
-600
-400
-200
0
200
400
600
distance (nm)
-4
-2
0
2
4
H
y
odd
even
a=100nm
-600
-400
-200
0
200
400
600
distance (nm)
-1
-0.5
0
0.5
1
1.5
H
y
odd
even
a=30nm
Magnetic field

## Slide 6: Dispersion of Slab SPP’s
Long range plasmon (even)
Short range plasmon (odd)
a=12nm
Long range plasmon (even)
Short range plasmon (odd)
Electric field
Long range plasmon (even)
Short range plasmon (odd)
-600
-400
-200
0
200
400
600
distance (nm)
0
0.2
0.4
0.6
0.8
1
1.2
|
E
x
|

## Slide 7: Guiding Light with Long-Range Plasmons
MZI Sensor
Thermo optic attenuator
The thermo-optic attenuator depicted here consists of a metal stripe sandwiched between a layer of SiO2 and a polymer having different thermo-optic properties. At room temperature, the long-range plasmon can propagate because the chosen polymer is index-matched to SiO2. When the temperature rises, the index of the polymer becomes different than that of the SiO2. The resulting asymmetry strongly attenuates the mode, which becomes radiative

## Slide 8: Gap (slot) SPP
Inside the dielectric gap
In the metal cladding
Longitudinal electric field
Boundary condition –continuous Ez
Introduce
For odd mode
Skin depth
x
0
+a/2
-a/2
z
y
Ex

## Slide 9: Gap SPP
Gold with air gap
W=1
W=0.5
W=0.25
W=0.1
even
odd
Odd solution does not exist!
As long as
Graphic solution
The effective index of gap mode neff=β/k0 has a very weak frequency dependence for as long as gap is larger than skin depth

## Slide 10: Gap SPP
λ=1500nm
λ=1000nm
λ=750nm
λ=600nm
λ=1500nm
λ=1000nm
λ=750nm
λ=600nm
Magnetic field
λ=750nm
-150
-100
-50
0
50
100
150
distance (nm)
0
0.2
0.4
0.6
0.8
1
1.2
E
x
Electric field
λ=500nm, 750nm,1000nm
This is a standard TEM wave in a metal transmission line –it has very little to do with a “real” plasmon

## Slide 11: Where is the odd solution?
Inside the dielectric gap
In the metal cladding
Longitudinal electric field
Boundary condition –continuous Ez
Introduce
For odd mode
x
0
+a/2
-a/2
y

## Slide 12: Other TM solutions
TM1
(odd)
TM2
(even)
No TM0!!!
Solutions are all close to normal metal waveguide modes
Round trip phase delay of 2mπ
Instead of TM0 there exists TEM wave – a very special wave indeed.
λ=700nm
TM1
TEM
cutoff
Must be real

## Slide 13: Plasmonic circuits

## Slide 14: Confinement vs. Loss

## Slide 15: Confinement vs. Loss

## Slide 16: Plasmonic nanolasers

## Slide 17: Plasmonic modulators

## Slide 18: Hybrid mode modulator